Technical Data Sheet

AirTight Sprayfoam 2.0 lb

Product Description

Airtight closed cell rigid polyurethane foams are technically advanced, low viscosity, two component systems specifically designed for spray operations to produce rigid polyurethane wall foam insulation. Air Tight closed cell was developed using an EPA approved, zero ozone-depleting next generation blowing agent.  Properly installed, the finished foam insulation adheres tenaciously to wood, metal, concrete & most common construction materials.

Credentials and Certifications

ASTM E-84 Class 1                                                                  NFPA 286

SPF Maximum Thickness                         4 inches                   8 inches in wall

Flame Spread			…. < 10                           12 inches in ceiling

Smoke Development		…. < 450                         with installed 15 min. thermal barrier

Typical Properties

Mix Ratio Parts by Weight				1:1 A component to B component

Cream Time					2-3 seconds

Tack Free Time					7-8 seconds

Rise Time					12-14 seconds

Core Density					1.55 +/- .05 pcf

Viscosity at 73 Degrees F				250 cps “B” component

Physical Properties

Property						Test Method			Value

In Place Density					ASTM D – 1622			2.0 lbs

Compressive Strength				ASTM D – 1621			35 psi

Tensile Strength					ASTM D – 1623			80 psi

Shear Strength					ASTM C – 273			35 psi

Closed Cell Content				ASTM D – 6226			>90%

R-Value per inch					ASTM C – 518			6.3

Water Vapor Transmission			ASTM E – 96			<1 @ 2 inches

Air Permability					ASTM E – 283-04

Polyurethane foam systems should not be left exposed in interior applications & must be protected by a minimum 15-minute thermal barrier between conditioned habitable space & uninhabitable space.

AirTight Marketing & Distribution, Inc.

145 Newborn Road

Rutledge, GA  30663

800.995.9466